## Slide 1: Chitosan-based in-situ gelling systems for intravesical drug delivery
References
Zhou et al., 2015, ‘Glycerophosphate-based chitosan thermosensitive hydrogels and their biomedical applications’, Carbohydrate Polymers 117 (2015), pp. 524-536.
Abdel-Bar et al., 2014, ‘Defining cisplatin incorporation properties in thermosensitive injectable biodegradable hydrogel for sustained delivery and enhanced cytotoxicity’, IJP 477 (2014), pp. 623-630
Rheological studies – Viscoelastic properties
Temperature ramp 5-60oC, ramp rate 1oC/min, frequency 1Hz, strain 1% for gelation temperature (GT) determination: 25oC < GT ≤ 37oC optimal for IDD.
Figure 4 Evolution of G’ & G” for CH/ß-GP system with temperature increase from 5oC to 60oC.
- Frequency sweep from 0.1to 10Hz at temperature of 37oC and strain 1%: The greater the rate of increase of storage modulus (G’) relative to loss modulus (G”) at 1Hz, the weaker the strength of the gels.
Figure 5 Frequency dependent changes (0.1-10Hz) of the viscoelastic properties of CHGP thermogelling systems at 37oC.
-Time sweep at constant temperature of 37oC (strain 1%, frequency 1Hz): Gelation time identified as point of deflection of G’.
Figure 6 Time dependent changes of the viscoelastic properties of CHGP thermogelling systems at 37oC.
Conclusion:
  This work suggests that the molecular weight of chitosan is the critical parameter for their gelation at 37oC. This is because LCH/ß-GP and MCH/ß-GP with pH of 7.2-7.35 did not form sustained gel within 1 h. LCH/ß-GP and MCH/ß-GP may be viable delivery vehicles for other areas of drug delivery where fast onset of in situ gelation is not desirable. HCH/ß-GP systems appears suitable for the intravesical administration of anticancer drugs for therapy of bladder diseases.
Future work:
Gelation and rheological properties of HCHGP hydrogel diluted with artificial urine will be investigated in order to evaluate its resistance to the effect of human urine in situ. Also, syringeability, adhesive and compressibility testing using texture analyser will be carried out to determine its ease of transit through the cathether to the bladder.
Contact information
Oluwadamilola M. Kolawole
Department of Pharmacy, University of Reading, Whiteknights, RG6 6AH
Email: o.m.kolawoleneealuko@reading.ac.uk
Introduction
The urothelium (bladder permeability barrier) makes the bladder impermeable to drug thereby hindering therapeutic success of bladder diseases.
Conventional intravesical treatment (usually in solutions) for bladder cancer are prone to wash-off and dilute by the urine.
Figure 1 Schematic diagram showing intravesical delivery to the human bladder.
Chitosan/β-glycerophosphate (CH/ß-GP) systems could potentially improve drug residence time in a sustained release pattern because they are mucoadhesive liquid which transform into gel at physiological temperature of 37oC, making them resistant to the influence of urine. They have not been explored for intravesical drug delivery (IDD) despite considerable successes in other areas of drug delivery and tissue engineering (Zhou et al., 2015).
Method:
Figure 2: Preparation of aqueous solution of chitosan/ß-glycerophosphate thermogelling systems.
The formulations were studied using water bath (37oC) for 1h. Their viscoelastic properties were also assessed using Rheometer scanned from 5-60oC as well as maintained at 37oC at strain 1% and frequency 1Hz.
Results / Discussion:
Gelation studies using water bath (37oC): Gelation time (Gt) ≤ 20 mins desirable for IDD
Figure 3: Gelation process of chitosan/ß-glycerophosphate thermogelling system (from 25 to 37oC)