## Slide 1: Production of levulinic acid from sugarcane bagasse
L.D. Mthembu, L. M. Schmidt, P. Reddy, I. Smirnova and N. Deenadayalu

## Slide 2: Outline
Aim
Objectives of the study
Introduction
Methodology
Results and Discussion
Conclusion
Acknowledgements

## Slide 3: Aim
The main purpose of this work was to produce levulinic acid from sugarcane bagasse using an experimental design that complies with the principles of Green Chemistry.
Green chemistry, which is also known as sustainable chemistry, is the design of chemical products and processes that reduce or eliminate the use or generation of hazardous substances. Green chemistry applies across the life cycle of a chemical product, including its design, manufacture, and use.
Prevention
Use of Renewable Feedstocks
Less Hazardous Chemical Syntheses

## Slide 4: Objectives of the Study
Sugarcane bagasse pretreatment:
Liquid Hot Water pretreatment
Enzymatic hydrolysis
Acid hydrolysis of glucose solution:
Comparing sulphuric acid and methanesulfonic acid (MSA)
Optimisation of levulinic acid production:
Comparing parameters such as temperature, time and acid concentration

## Slide 5: Introduction
When the sugarcane stems are milled to obtain the cane juice, which is used for sugar production, the residual fraction that is left after the extraction of juice is called sugarcane bagasse (SB).
Sugarcane is mainly used for sugar and alcohol production.
Sugarcane bagasse is used as a fuel to power the sugar mill, when burnt. It produces sufficient heat energy to supply all the needs of a typical sugar mill. What is good about the SB used for sugar mill electricity production is that the resulting CO2 emissions are equal to the amount of CO2 that the sugarcane plant absorbed from the atmosphere during its growing phase, which makes the process of cogeneration a greenhouse gas neutral technology(Rainey 2009).

## Slide 6: Sugarcane Bagasse (SB)
Effect of pretreatment on SB
Composition analysis of SB
Source: Alonso et al. 2010
Source: Kumar et al. 2009

## Slide 7: Levulinic Acid
Levulinic acid (LA) (4-oxopentanoic acid) also known as 3-acetypropionic acid, is a linear C5-alkyl carbon chain containing one carboxylic acid group in position 1 and one carbonyl group in position 4. The structure of LA is given in Fig. 1.
Figure 1. Molecular structure of levulinic acid

## Slide 8: Levulinic Acid Applications
Source: Avantium.com

## Slide 9: LA market volume share by applications
Chart: 
| Pharmaceuticals | Agriculture | Food addictive | Cosmetics
 | 0.232 | 0.428 | 0.21 | 0.13
Source: Grandviewresearch.com

## Slide 10: Methodology
LHW Pretreatment
3 L reactor
1 kg of pelletized bagasse
Temp.: 200 °C
Time: 30 min
Volume flow: 250 ml/min
Enzymatic hydrolysis
10 L glass reactor
Bagasse/water: 1:10
Temp.: 50 °C
Time: 72 hr.
pH: 4.8
Enzyme activity: 15 FPU (Cellic Ctech 2)

## Slide 11: Levulinic Acid Production
Glucose solution
30 ml reactor
Substrate: 0,24 M (glucose solution, pure glucose, glucose/xylose, fructose)
Temp.: 180 °C
Time: 45 min.
Catalyst: 0,5 M (H2SO4, MSA)
Cellulignin
30 ml reactor
Substrate: 1,7 wt% (Cellulignin, pure Cellulose)
Temp.: 150 °C
Time: 120 min.
Catalyst: 1 M (MSA)

## Slide 12: Results and Discussion
Chart: Main componets
Chart: Compositional analysis of sugarcane bagasse
| Cellulose | Hemicellulose | Lignin (total) | Residue
 | 40.01 | 25.29 | 24.6 | 10.1

## Slide 13: LHW pretreatment for sugarcane bagasse
Chart: Cellulignin
| Cellulose | Hemicellulose | Lignin | Rest
Cellulose Hemicellulose Lignin (total) Residue | 56 | 11.1 | 28.71 | 4.19

## Slide 14: Hydrolysate from LHW
 | Monomer (mg/L) | Oligomers (mg\L)
Cellobiose | <50 | 460
Glucose | 115 | 1200
Xylose | 1400 | 21300
Arabinose | 1100 | 2300
Formic acid | <50 | <100
Acetic acid | 1100 | 3700
Levulinic acid | <50 | <100
HMF | <50 | <100
Furfural | 370 | 570
Hydrolysate
pH value: 3.83
Density: 1.012 g.cm-3 at 20 °C
Table 1: Hydrolysate composition from LHW

## Slide 15: Enzymatic hydrolysis
Chart: lignin
| Cellulose | Hemicellulose | Lignin | Rest
Cellulose Hemicellulose Lignin (total) Residue | 39.4 | 5.38 | 50.41 | 4.81

## Slide 16: Glucose solution
 | Monomers (mg/L) | Oligomers (mg\L)
Cellobiose | 1500 | 730
Glucose | 42800 | 44000
Xylose | 9600 | 11700
Arabinose | 500 | 600
Formic acid | 500 | 0.0
Acetic acid | 2600 | 0.0
Levulinic acid | <50 | 0.0
HMF | 60 | 160
Furfural | 400 | 550
Table 2: Compositional analysis of the liquid fraction obtained after enzymatic hydrolysis
Test for glucose solution
DNS for reducing sugars: 52.2 g/L
Glucose kit : 42.7 g/L
Xylose kit : 9.03 g/L

## Slide 17: Table 3: Glucose solution and other substrate hydrolysed with H2SO4 to produce LA
No. | Sample | Cellobiose | Glucose | Xylose | Arabinose | Formic Acid | Acetic Acid | Levulinic acid | HMF | Furfural
 |  | mg/l | mg/l | mg/l | mg/l | mg/l | mg/l | mg/l | mg/l | mg/l
1 | Fructose | < 50 | < 50 | < 50 | < 50 | 8100 | 340 | 17700 | < 50 | < 50
2 | Glucose | < 50 | < 50 | < 50 | < 50 | 6875 | 265 | 14450 | < 50 | < 50
3 | Glucose and xylose | < 50 | 185 | 75 | < 50 | 7600 | 305 | 15000 | < 50 | 235
4 | Glucose Solution | < 50 | 240 | 180 | 65 | 8550 | 2825 | 15900 | < 50 | 290

## Slide 18: Acid hydrolysis (sulphuric acid) of the glucose solution
Chart: LA production from SB using sulphuric acid
| Fructose | Glucose | Glucose and Xylose | Glucose solution
Conversion rate % | 100 | 99.8 | 99.6 | 99.4
LA Yield % | 41.4 | 33.8 | 35 | 37.2

## Slide 19: Table 4: Glucose solution and other substrate hydrolysed with MSA to produce LA
No. | Sample | Cellobiose | Glucose | Xylose | Arabinose | Formic Acid | Acetic Acid | Levulinic acid | HMF | Furfural
 |  | mg/l | mg/l | mg/l | mg/l | mg/l | mg/l | mg/l | mg/l | mg/l
1 | Fructose | < 50 | < 50 | 70 | < 50 | 8025 | 355 | 17450 | < 50 | < 50
2 | Glucose | < 50 | 725 | 65 | < 50 | 6725 | 230 | 13800 | <50 | < 50
3 | Glucose and xylose | < 50 | 160 | 105 | < 50 | 7050 | 295 | 13650 | < 50 | 260
4 | Glucose Solution | < 50 | 275 | 225 | < 50 | 8175 | 2775 | 14900 | < 50 | 290

## Slide 20: Acid hydrolysis (MSA) of the glucose solution
Chart: LA production from SB using MSA
| Fructose | Glucose | Glucose and xylose | Glucose solution
Conversion rate % | 100 | 98.3 | 99.7 | 99.4
LA Yield % | 40.9 | 32.4 | 32 | 34.9

## Slide 21: Design of Experiments (DoE)
Stat-Ease Design-Expert 8.0.7.1 was used for the experimental design and analysis. Set-up and analysis of the designs were conducted according to the standard procedure implemented in the software. DoE provides a set of powerful tools for the effective planning and evaluation of experimental designs by minimizing the number of required experiments
Parameter | Minimum | Maximum
Temperature | 160 °C | 200 °C
Reaction time | 30 min | 90 min
Acid | 0.25 M | 1.0 M
Table 5: Parameters used for optimization LA production

## Slide 22: Table 6 (a) : Optimization of LA production
Run | Temperature [ oC] | Time [min] | Acid [M] | Levulinic acid (mg/L)
1 | 180 | 60 | 0.131 | 11000
2 | 180 | 60 | 0.625 | 16000
3 | 160 | 90 | 0.250 | 11000
4 | 153.7 | 60 | 0.625 | 12000
5 | 160 | 90 | 1.000 | 17000
6 | 200 | 30 | 1.000 | 16000
7 | 180 | 60 | 0.625 | 16000
8 | 180 | 99.5 | 0.625 | 18000
9 | 180 | 60 | 0.625 | 17000
10 | 200 | 30 | 0.250 | 16000
11 | 180 | 60 | 0.625 | 16000
12 | 206.3 | 60 | 0.625 | 16000
13 | 180 | 20.5 | 0.625 | 16000
14 | 160 | 30 | 1.000 | 12000
15 | 180 | 60 | 0.625 | 19000
16 | 200 | 90 | 0.250 | 15000
17 | 160 | 30 | 0.250 | 3000
18 | 180 | 60 | 1.119 | 16000
19 | 200 | 90 | 1.000 | 17000
20 | 180 | 60 | 0.625 | 17000

## Slide 23: Table 6 (b): Optimization of LA production
Sample | Cellobiose | Glucose | Xylose | Arabinose | Formic acid | Acetic acid | Levulinic acid | HMF | Furfural
 | mg/l | mg/l | mg/l | mg/l | mg/l | mg/l | mg/l | mg/l | mg/l
431 | 170 | 14500 | 930 | < 50 | 5900 | 290 | 11000 | 810 | 2300
432 | < 50 | < 50 | 210 | < 50 | 7400 | 290 | 16000 | < 50 | < 50
433 | 140 | 16500 | 930 | < 50 | 6000 | 290 | 11000 | 560 | 1800
434 | 220 | 15000 | 800 | < 50 | 5700 | 260 | 12000 | 410 | 1300
435 | < 50 | 370 | 190 | < 50 | 7900 | 280 | 17000 | < 50 | < 50
436 | < 50 | < 50 | 160 | < 50 | 6400 | 300 | 16000 | < 50 | < 50
437 | < 50 | < 50 | 250 | < 50 | 7400 | 280 | 16000 | < 50 | < 50
438 | < 50 | < 50 | 230 | < 50 | 7600 | 300 | 18000 | < 50 | < 50
439 | < 50 | < 50 | 230 | < 50 | 7800 | 290 | 17000 | < 50 | < 50
440 | 95 | 260 | 260 | < 50 | 7800 | 300 | 16000 | < 50 | 860
441 | < 50 | < 50 | 210 | < 50 | 7900 | 300 | 16000 | < 50 | < 50
442 | < 50 | < 50 | 190 | < 50 | 4700 | 320 | 16000 | < 50 | < 50
443 | < 50 | < 50 | 160 | < 50 | 7800 | 290 | 16000 | < 50 | < 50
444 | < 50 | 13000 | 670 | < 50 | 5600 | 270 | 12000 | 360 | 1400
445 | < 50 | < 50 | 180 | < 50 | 8500 | 300 | 19000 | < 50 | 130
446 | < 50 | < 50 | 220 | < 50 | 6500 | 310 | 15000 | < 50 | < 50
447 | 575 | 33500 | 5160 | 529 | 2300 | 270 | 3000 | 920 | 2400
448 | < 50 | < 50 | 170 | < 50 | 7100 | 300 | 16000 | < 50 | < 50
449 | < 50 | < 50 | 130 | < 50 | 3700 | 310 | 17000 | < 50 | < 50
450 | < 50 | < 50 | 170 | < 50 | 7800 | 300 | 17000 | < 50 | < 50

## Slide 24: Production of LA from cellulignin
No. | Sample | Cellobiose | Glucose | Xylose | Arabinose | Formic Acid | Acetic Acid | Levulinic acid | HMF | Furfural
 |  | mg/l | mg/l | mg/l | mg/l | mg/l | mg/l | mg/l | mg/l | mg/l
1 | Cellulignin (LHW) | < 50 | 1075 | < 50 | < 50 | 940 | 215 | 1875 | < 50 | < 50
2 | Cellulose (pure) | < 50 | 2400 | <50 | < 50 | 1625 | 65 | 3250 | < 50 | < 50
Table 7: Production of LA from cellulignin and pure cellulose using MSA

## Slide 25: Conclusion
LHW dissolved hemicellulose although 11 % of hemicellulose remained in cellulignin, this method is more preferred because it only uses water and the reaction time of 1 hr.
Enzymatic hydrolysis converted cellulose into glucose solution with a concentration of 42.7 g/L.
In comparing sulphuric acid and MSA, a slightly difference of 2.3 % was observed, therefore MSA can be used for the production of LA because it is more environmentally friendly, less toxic and less corrosive compared to H2SO4.
When LA was produced from glucose solution at 180 oC, with 0.625 M of MSA for 60 min, gave the highest yield of 19000 mg\L compared with other parameters that were used for the optimisation of LA production.

## Slide 26: Acknowledgements
I would like to thank the following for assisting me in this work:
My supervisor, Prof Nirmala Deenadayalu and Co-supervisor, Dr Prashant Reddy
Lisa Schmidt , Dr Carsten Zetzl and Prof Irina Smirnova from TUHH
Alpha and Omega
My family
Technische Universität Hamburg-Harburg (TUHH) , Institute of Thermal Separation Processes for providing the facilities to carry out the present work
And NRF for funding this project
DUT for providing me with the opportunity to pursue my studies

## Slide 27: Thank you for listening Ngiyabonga